## Slide 1
COMPOSITE DAMAGE TOLERANCE (CDT)
Residual strength after BVID impact
Guillermo Balsalobre Carmona
Julio de 2025

## Slide 2
Index:
BVID impact criterion
Design values
Suggestion for future CDT analyses
CDT module of SAM software
Case study
References

## Slide 3
· BVID – Barely Visible Impact Damage. It is the damage in a composite laminate
consequence of a low velocity impact at the threshold of (visible) detectability.
Residual strength after BVID impact criterion:
· Transversal and Edge impact:
· Low energy impact (typ. E=35J)

## Slide 4
Design values:
TAI: Tension After Impact, as allowable strain
CAI: Compression After Impact, as allowable strain
BAI: Bending After Impact, as allowable strain
Sketch of impacted laminates (tension & compression)

## Slide 5
TAI allowable is a constant material property.
Same B-basis value for all conditions.
TAI: Tension After Impact, as allowable strain:
TAI allowable takes minimum values are not affected by the temperature.
BAI: Bearing After Impact, as allowable strain:
Depends on material. Can be calculated, but for IMA-M21E_UD Tape, and in the absence of more precise test data, TAI is used as cut-off value for BAI.
Airbus DS approximation: TAI is a fixed value for each material, independent of fibre directionality or thickness.
IMA-M21E_UD Tape

## Slide 6
CAI: Compression After Impact, as allowable strain:
CAI is modelled with sensitivity to fibre directionality and laminate thickness.
Three values of CAI are used based on stacking angles (0º, ±45º, 90º):
· One to compare with strain in plies at 0º:
· Another one to compare with strain in plies at 45º:
· Finally, another to compare with strain in plies at 0º:
in order to calculate RF in each direction as shown:
Sketch with static margins for all ply directions in a plate under bi-axial compression

## Slide 7
CAI depends on impact energy, material - elastic modulus of material and of direction of interest, thickness of each fibre direction, temperature…
CAI: Compression After Impact, as allowable strain:
CAI allowable increase with the laminate thickness and there is a reduction of the allowable value with the Temperature
IMA-M21E_UD Tape
Each laminate needs 3 CAI calculations… CDT software

## Slide 8
CDT module of SAM software:
SAM software: “Structural Analysis Method” is a Airbus DS software for performing different types of structural analysis using experimental stress methods under development.
module CDT: “Composite Damage Tolerance” for residual strength after BVID impact analysis

## Slide 9
Case study:
Falcon 10X
Fittings HTP (Box and Elevator) & VTP (Box and Rudder)
CDT analysis on Spar and Skin surroundings of fittings
Each location: HF1-HF6 (2 of them with 2 extra Fail safe cases), +Fy/-Fy, Cold/Hot

## Slide 10
Pre processing:
Hypermesh Matrix Browser
from DFEM forces results
Excel postprocessing in HF1_Loads_COLD_CDT.xls
CDT Load Input “.sal”
*results in material system

## Slide 11
Pre processing:
Hypermesh Matrix Browser
from DFEM forces results
Excel postprocessing in “HF1_Loads_COLD_CDT.xls”
CDT Load Input “.sal”
(*) sign of moments are inverted
Reorder in SAM format
(*)

## Slide 12
excelpreprocessing
Inputs:
“SAM_CDT_HF1_COLD.dat”
“HF1_Loads_COLD_CDT.sal”

## Slide 13
Outputs:
“SAM_CDT_HF1_COLD.out”
“SAM_CDT_HF1_COLD.aux.out”

## Slide 14
“SAM_CDT_HF1_COLD.out” ,“SAM_CDT_HF1_HOT.out”, … (para FY/-FY, FS…)
“CDT_HF1-RF_Results.xlsx”
Post processing:

## Slide 15
Post processing:
“SAM_CDT_HF1_COLD.aux.out” & “…HOT.aux.out”
“CDT_HF1_RF_Results.xlsx”

## Slide 16
Suggestions for future CDT analyses:
· Preprocessing automatization: Directly from “.op2” results, obtain “loads.sal” input for CDT analysis with python
Avoid mistakes with Matrix Browser: license dependent and sometimes hace lo que le da la gana.
Saving time in preprocessing excel preparation: each fitting HFx_Loads_COLD_CDT.xlsx rows & columns must be updated manually depending on number of elements and loadcases.
¿?

## Slide 17
Again, saving time in postprocessing excel preparation, where each fitting CDT_HFx_RF_Results.xlsx must be updated depending on number of elements and loadcases.
Instead of this, obtain ONLY needed information directly from “.aux.out”
Suggestions for future CDT analyses:
· Postprocessing automatization: Postprocessing all results from “.aux.out” directly with python

## Slide 18
References:
· TEAS-NT-1910014-J: Material Design Values and Methods for Structural Analysis of the Future Falcon
· TEA-T-NT-190111-J_SAM: SAM Stress Software User’s Reference Manual
· SMM_section1.4_chapter1451_CFRP_IMA-M21E-UD